β-1,4-葡聚糖硫酸酯的制备及其抗凝血活性

王兆梅，李  琳，郭祀远，肖凯军

(华南理工大学轻化工研究所，广东广州510640)

摘 要： 对微晶纤维素（MCC）进行硫酸酯化修饰，得到多种β-1,4-葡聚糖硫酸酯（GS），其硫酸取代度（Ds）在1.10～1.70范围内。选择Ds为1.70的GS用于结构分析和抗凝血活性研究。IR分析表明，MCC通过硫酸化反应引入了硫酸酯基13C NMR揭示，硫酸酯化主要发生在C6，部分在C2，而C3位不发生硫酸酯化反应。凝血分析表明，0.2mg/L的GS即可显著延长血浆的活化凝血活酶时间(tAPTT)和凝血酶时间(tTT)，使血浆tAPTT延长两倍，所需GS的剂量为0.7mg/L，低于活性为150IU/mg的肝素，在一定质量浓度范围内，GS的体外抗凝血活性与肝素相当。显色分析揭示，GS的抗凝血机制主要在于通过抗凝血酶AT-Ⅲ的调节作用抑制凝血因子Ⅱa和Xa的活性。



关键词： 葡聚糖硫酸酯；抗凝血；机制

中图分类号：TQ35;O614      文献标识码：A      文章编号：0253-2417(2006)04-0001-05

Preparation and Anticoagulation Activity of β1,4Glucan Sulfate

WANG Zhaomei, LI Lin, GUO Siyuan, XIAO Kaijun

(Research Institute of Light Industry and Chemical Engineering,South China University of Technolage, Guangzhou 510640, China)

Abstract: Various β1,4glucan sulfates(GS) were synthesized by sulfate of microcrystalline cellulose. Their sulfate substitute degree(Ds) varied in the range of 1.10 to 1.70.GS with Ds of 1.70 was selected for structural analysis and anticoagulation investigation.IR spectra showed the introduction of sulfate groups by sulfation.13C NMR indicated that sulfation occurred mainly at C6, partially at C2 and no sulfate substitution occurred at C3. Coagulation assays showed that 0.2 mg/L GS could significantly prolong tAPTT and tTT in plasma.The dosage of GS required to double tAPTT of normal human plasma was 0.7 mg/L, lower than that of heparin with the anticoagulation activity of 150 IU/mg. Its potent of anticoagulation in vitro reached the efficacy of heparin in definite range of concentration. Chromogenic analysis revealed that the anticoagulation mechanism of GS was mainly due to the inhibition of the coagulation factors Ⅱa & Xa activities mediated by antithrombin ATⅢ.



Key words: glucan sulfate;anticoagulation;mechanism

E1级胶合板用脲醛树脂的13C NMR定量分析

金立维，王春鹏，周道兵，储富祥*，赵临五

（中国林业科学研究院林产化学工业研究所；国家林业局 林产化学工程重点开放性实验室，江苏南京210042）

摘 要： 采用13C NMR定量分析了由选定碱-酸-碱工艺所合成的E1级胶合板用脲醛树脂。结果表明：在初始碱性阶段有70.27 %的甲醛分子转化成了羟甲基脲，24.83 %的甲醛分子转化成了亚甲基醚键。在随后的酸性缩聚阶段中，64 %的羟甲基脲发生断裂，放出甲醛，缩聚成亚甲基键及亚甲基醚键。在酸性阶段加入的第二批尿素与树脂中的游离甲醛形成羟甲基脲。超过一半的亚甲基醚键在最后的碱性保温阶段发生分解，并与此时加入的第三批尿素生成羟甲基脲。



关键词： 脲醛树脂；羟甲基脲；亚甲基醚；胶合板



中图分类号：TQ323；TQ433     文献标识码：A      文章编号：0253-2417(2006)04-0006-05

Quantitative 13C NMR Analysis of Urea-formaldehyde Resin for E1-type Plywood

JIN Liwei, WANG Chunpeng, ZHOU Daobing, CHU Fuxiang, ZHAO Linwu

(Institute of Chemical Industry of Forest Products,CAF; Key and Open Lab.on Forest Chemical Engineering,SFA, Nanjing 210042, China)

Abstract: The ureaformaldehyde(UF) resins for E1type plywood synthesized by specific procedure were quantitatively examined by the 13C NMR spectroscopy. It was proved that 70.27 % of formaldehyde molecules were transformed into hydroxymethylurea and 24.83 % formaldehyde molecules were transformed into methyleneether bond during the initial alkaline reaction stage（pH value 7.2-7.8）.About 64% of hydroxymethyl groups formed in the initial alkaline reaction stage were polymerized during the subsequent acidic reaction stage（pH value 5.4-5.6）by forming methylene or methyleneether bonds and releasing some formaldehyde. The free formaldehyde of resin could react with the second dosage of urea during the next acidic reaction stage（pH value 6.5-6.9） to form hydroxymethylureas. More than half of methyleneether bonds were decomposed during the last alkaline cooling stage（pH value 7.5-8.0）and reacted with the third dosage of urea to form hydroxymethylurea.



Key words:  ureaformaldehyde resin;hydroxymethylurea;methyleneether;plywood

AH型非贵金属催化松香歧化反应动力学研究

王亚明， 王路辉， 蒋丽红， 王 震

(昆明理工大学生物与化学工程学院，云南昆明650224)



摘 要： 用AH型非贵金属催化剂催化松香歧化反应，考察了搅拌速率、催化剂粒度、反应温度、反应时间对反应的影响，建立了动力学方程。确认在240～270℃范围反应为一级,求出在240、250、260和270℃时的反应速率常数分别为2.9×10-3、3.1×10-3、1.42×10-2和2.51×10-2min-1。表观活化能E为184.80×103 kJ/mol，频率因子A =1.453×1016。



关键词： AH型非贵金属催化剂；松香歧化反应；动力学方程

中图分类号：TQ351.47；TQ426    文献标识码：A    文章编号：0253-2417(2006)04-0011-03

Research on Reaction Kinetics of Disproportionation of Gum Rosin Catalyzed by AH Nonnoble Metal Catalyst

WANG Yaming, WANG Luhui, JIANG Lihong, WANG Zhen

(Institute of Biological and Chemical Engineering,Kunming University of Science and Technology, Kunming 650224, China)

Abstract: The reaction of disproportionation of gum rosin catalyzed by AH nonnoble metal catalyst was studied, and the effects of reaction temperature, reaction time, particle size of catalyst, and stir speed were investigated. It was found that the reaction was of the first order at 240-270℃. Reaction rate constants were 2.9×10-3, 3.1×10-3, 1.42×10-2, 2.51×10-2min-1 at 240, 250, 260 and 270 ℃,respectively. Apparent activation energy E was 184.80×103kJ/mol, frequency factor A was 1.453×1016.



Key words:  AH nonnoble metal catalyst；disproportionation of gum rosin；kinetic equation

FolinCiocalteu比色法测定橄榄中多酚含量的研究

何志勇，夏文水*

（江南大学食品学院，江苏无锡214036）



摘 要： 采用FolinCiocalteu比色法研究了橄榄多酚的定量测定方法。结果表明：橄榄多酚提取液在加入FolinCiocalteu试剂1.5 mL、10% Na2CO3 6 mL、反应时间2 h、温度30℃的条件下进行显色，并于765 nm处测定其吸光值，多酚质量浓度在7～70mg/L范围内与吸光值有良好的线性关系，根据此线性回归方程进行橄榄多酚的定量测定，该方法简单方便、稳定性好、准确度高。



关键词： 橄榄；多酚；比色法

中图分类号：TQ351.014      文献标识码：A      文章编号：0253-2417(2006)04-0015-04

Study on Determination of Polyphenol Content in Canarium album (Lour.) Rauesch. by FolinCiocalteu Colorimetry

HE Zhiyong, XIA Wenshui

(School of Food Science and Technology,Southern Yangtze University, Wuxi 214036, China)

Abstract: A quantitative determination method of polyphenol from Canarium album (Lour.) Rauesch. was studied by FolinCiocalteu colorimetry. The results showed that polyphenol content of C. album could be well calculated according to their colorimetric absorption at 765nm by applying FolinCiocalteu reagent 1.5mL and 10% Na2CO3 6 mL,2 h at 30℃ for colorimetric reaction, and the linear range of standard curve was 7-70mg/L.The method established was very convenient, stable and accurate.



Key words:  Canarium album (Lour.) Rauesch.;polyphenol;colorimetry

雷公藤抗肿瘤三萜成分的研究

杨光忠1，李援朝2

（1.中南民族大学生命科学学院民族药物研究所，湖北武汉430074；2.中国科学院上海生命科学院上海药物所，上海201203）



摘 要： 研究雷公藤根心部分的化学成分。采用硅胶柱色谱法进行分离，从其氯仿提取物中分得9个三萜化合物，经波谱分析鉴定为雷公藤素D（1）, 雷公藤素E （2）,直楔草酸（3）, 雷公藤素H（4）, 22-β-羟基-3-氧代-12-齐墩果烯-29-羧酸（5）, 雷公藤三萜酸C(6), 雷公藤素G（7）,  雷公藤酸A（8）, 雷公藤醇A（9）。抗肿瘤生物活性体外筛选实验表明：化合物7和9对P-388小鼠白血病细胞株的生长表现出强的抑制率，化合物1对A-549人肺腺癌表现出强的抑制率。



关键词： 卫矛科；雷公藤；三萜;抗肿瘤生物活性

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0019-04

Antitumor Triterpenoids from Tripterygium wilfordii Hook. f.

YANG Guangzhong1, LI Yuanchao2

(1. National Medicine Institute,College of Life Sciences,South Central University for Nationalities, Wuchang  430074, China;2. Shanghai Institute of Materia Medica,Shanghai Institute for Biological Sciences,Chinese Academy of Sciences, Shanghai 201203, China)

Abstract: To study the active principles of Tripterygium wilfordii Hook. f., nine triterpenoids were isolated from this plant by column chromatography with silica gel. Their structures were identified as triptotin D(1),triptotin E(2),orthosphenic acid (3),triptotin H(4),22βhydroxy3oxoΔ12oleanen29oic acid (5),triptotri

terpenic acid C(6), triptotin G(7),  wilforic acid A(8) and wilforol A(9). Compounds 7 and 9 showed strong inhibition against P388 rat leukaemia cell line. Compound 1 showed strong inhibition against A549 adenocarcinoma cell of lung.

Key words: Celastraceae;tripterygium wilfordii Hook. f.; triterpenoids;antitumor bioactivities

红花忍冬的三萜类成分研究

钱正明, 李会军, 李 萍*, 贺清辉, 齐芳芳

（中国药科大学生药学教研室；现代中药教育部重点实验室，江苏南京210038）



摘 要： 对红花忍冬地上部分进行化学成分研究。分离鉴定了5个三萜类化合物：葳岩仙皂苷 C(1)、木通皂苷 D(2)、木通皂苷 F(3)、熊果酸(4)和常春藤皂苷元(5)。经文献检索，5个化合物均为首次从该种植物中分离得到，其中化合物4系首次从该属植物中分得。



关键词： 红花忍冬；三萜

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0023-03

Triterpenoids from the Aerial Parts of Lonicera syringantha Maxim.

QIAN Zhengming, LI Huijun, LI Ping, HE Qinghui, QI Fangfang

(Department of Pharmacognosy; China Pharmaceutical University and Key Laboratory of Morden Chinese Medicines,Ministry of Education, Nanjing 210038，China)

Abstract: Triterpenoids from the aerial parts of Lonicera syringantha Maxim. were studied. Five triterpenoids were isolated and their structures were identified to be cauloside C (1)，akebiasaponin D (2)，akebiasaponin F (3)，ursolic acid (4) and hederagenin (5). Compound 4 was isolated from the genus Lonicera for the first time and all 5 compounds were first isolated from the species of this plant.

Key words: Lonicera syringantha Maxim.;triterpenoids

负载铜活性炭催化剂制备及催化氧化印染废水

李伟峰1 ，祝社民2 ，宋天顺1，陈 佯1 ，陈英文1，沈树宝1*

(1.南京工业大学制药与生命科学学院,江苏 南京210009;2.南京工业大学材料科学与工程学院,江苏 南京210009)

摘 要： 对以ClO2氧化印染废水用的负载铜活性炭催化剂制备工艺进行了研究。实验结果表明：该催化剂的最佳制备工艺为：酸浸液浓度2.5mol/L,浸渍12h；硝酸铜浸渍液质量分数7.5 %，浸渍后活性炭先室温干燥，后80℃烘干，再在280℃下焙烧3h。并通过对实际印染废水的处理确定了最佳催化氧化工艺。失活催化剂经再生处理，可恢复约90%的催化活性。



关键词： 二氧化氯；活性炭；催化氧化；印染废水

中图分类号：TQ426;O643.3    文献标识码：A     文章编号：0253-2417(2006)04-0026-05

Preparation and Application of Copperloaded Activated Carbon Catalyst for  Catalytic Oxidation of Dye Wastewater

LI Weifeng1， ZHU Shemin2， SONG Tianshun1， CHEN Yang1， CHEN Yingwen1，SHEN Shubao1

(1.College of Life Science and Pharmacy,Nanjing University of Technology, Nanjing 210009, China;2.College of Material Science and Engineering,Nanjing University of Technology, Nanjing 210009, China)

Abstract: The catalyst, which is composed of activated carbon as carrier and loaded with copper oxide (CuO) as active component，was made and main factors in the preparation of this catalyst were further analyzed. Under the optimized preparation condition of nitric acid 2.5mol/L,soaking time 12h, concentration of Cu(NO3)2 7.5 %, calcination temperature 280℃ for 3h, the optimum catalytic activity could be obtained. The best catalytic oxidation process of dye wastewater treatment was also investigated by this catalyst. The regeneration process of deactivated catalyst was also investigated and the activity of regenerated catalyst was recovered to about 90%.



Key words:  chlorine dioxide;activated carbon;catalytic oxidation;dye wastewater

桐油酸酐酰亚胺环氧树脂耐热性研究

商士斌， 王 丹， 高 宏， 王定选



(中国林业科学研究院林产化学工业研究所;国家林业局 林产化学工程重点开放性实验室,江苏南京210042)

摘 要： 以桐油、双马来酰亚胺、马来酸酐及环氧树脂为基本原料,合成了具有较好耐热性的桐油酸酐酰亚胺环氧树脂。重点讨论了不同原料，如桐油、马来酐、双马来酰亚胺及环氧树脂的用量、固化反应温度及固化反应时间等因素对树脂耐热性的影响。当桐油、双马来酰亚胺、马来酐和环氧树脂的质量比为1∶0.25∶0.2∶0.4,150℃烘烤5h固化时，所得树脂具有较好的耐热性，温度指数(T20000)可达160.8℃。



关键词： 桐油；双马来酰亚胺；环氧树脂；马来酸酐；耐热性能

中图分类号：TQ323.5      文献标识码：A      文章编号：0253-2417(2006)04-0031-03

Thermal Stability of Bismaleimideepoxy Resin Modified by Tung Oilmaleic Anhydride Adduct

SHANG Shibin, WANG Dan，GAO Hong, WANG Dingxuan

(Institute of Chemical Industry of Forest Products,CAF；Key and Open Lab. on Forest Chemical Engineering，SFA, Nanjing 210042, China)

Abstract: A cured epoxy resin with high thermal stability was prepared from tung oil, a bismaleimide, maleic anhydride and an epoxy resin (E51). The effect of dosages of each component and the curing conditions were investigated. The optimum condition is as follows: weight ratio of tung oil/bismaleimide/maleic anhydride/E51 is 1∶0.25∶0.2∶0.4, curing temperature is 150 ℃ and curing time 5 h,the temperature index (T20000) of the resin is 160.8 ℃.



Key words:  tung oil；bismaleimide；epoxy resin；maleic anhydride;thermal stability

相思树硫酸盐浆无元素氯漂白性能的研究

邓拥军1，房桂干1*，李 萍1，刘君良2， 江泽慧2

（1.中国林业科学研究院林产化学工业研究所；国家林业局林产化学工程重点开放性实验室，江苏南京210042; 2.中国林业科学研究院木材工业研究所，北京100091）



摘 要： 系统对比研究了大叶相思、马占相思、厚荚相思及纹荚相思4种相思树硫酸盐法制浆性能及无元素氯（ECF）漂白性能。结果表明，采用硫酸盐法制浆，用碱量（氧化钠计）16 %、硫化度25%时，制得的4种相思树硫酸盐浆经OPDP1P2（OP为氧强化脱木质素，D为ClO2漂，P为H2O2漂）4段漂白，漂后纸浆的光学性能及强度性能优良。纸浆白度均达86.0%（ISO，以下同）以上，叩解度为30°SR时，抗张指数在55.8～60.7 N·m/g之间。4种相思树中大叶相思的制浆性能最优，马占相思和纹荚相思居中，厚荚相思的制浆性能最差。



关键词： 大叶相思；马占相思；厚荚相思；纹荚相思；硫酸盐浆；无元素氯漂白

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0034-05

Study on Elemental Chlorinefree Bleaching Properties of Kraft Pulp of Acacia  Wood Species

DENG Yongjun1, FANG Guigan1, LI Ping1, LIU Junliang2, JIANG Zehui2

(1.Institute of Chemical Industry of Forest Product,CAF;Key and Open Lab. on Forest Chemical Engineering,SFA, Nanjing 210042, China; 2. Research Institute of Wood Industry,CAF, Beijing 100091, China)

Abstract: Pulping and bleaching performances of 4 wood species(Acacia auriculiformis Willd.，A. mangium Willd., A. crassicarpa and A.aulacocarpa）were studied and the properties of these pulps were compared. The results showed that the screened yields of these kraft pulps were from 46.95% to 50.95%.By using elemental chlorinefree

(ECF)bleaching, all these bleached pulps had high ISO brightness and high physical properties,the brightness of these pulps could be bleached from 86.0 % to 89.2 %, ISO; on 30 °SR beating degree, the tensile indexes of these bleached pulps could reach from 55.8 to 60.7 N·m/g.The comprehensive kraft pulping potentials of these wood species were summarized that A.uriculiformis is the best one, A. mangium and A.aulacocarpa are in the middle,and A. crassicarpa is the worst.



Key words: Acacia auriculiformis Willd.;A. mangium Willd.;A.crassicarpa;A.aulacocarpa; kraft pulping; elemental chlorine free bleaching

固体超强酸催化长叶烯制备异长叶烯的研究

罗金岳1， 安鑫南1， 雷福厚2

（1．南京林业大学化学工程学院，江苏南京210037；2．广西民族大学化学与生态工程学院，广西南宁530006）

摘 要： 研究了SO42-/TiO2-ZrO2型固体超强酸催化剂的制备及其催化长叶烯的异构反应，通过GC、GC-MS和标样分析，确定其主产物为异长叶烯。结果表明，该催化剂对长叶烯的异构化反应有很高的催化活性和较好的选择性。考察了其催化性能的影响因素。结果表明，适宜的催化剂制备条件是：n(钛)∶n(锆)为3∶1，焙烧温度550℃。长叶烯异构优化的工艺条件：反应时间4h、反应温度165℃、催化剂用量4 %。该条件下长叶烯转化率99.1 %，异长叶烯得率97.2 %。同时考察了催化剂放置时间对异构产物的影响和催化剂重复使用情况。



关键词： 长叶烯；异长叶烯；固体超强酸；SO42-/TiO2-ZrO2催化剂

中图分类号：TQ351.471      文献标识码：A      文章编号：0253-2417(2006)04-0039-04

Study on Preparing Isolongifolene from Longifolene Catalyzed by Solid Superacid

LUO Jinyue1， AN Xinnan1， LEI Fuhou2

（1. College  of  Chemical  Engineering,Nanjing  Forestry  University,  Nanjing  210037, China；2. College of Chemistry and Ecology Engineering，Guangxi University for Nationalities， Nanning 530006，China)

Abstract: The reactions of　isomerization of longifolene catalyzed by SO42-/TiO2ZrO2 solid superacid are performed. From analyses of GC and GCMS, the main product is isolongifolene from isomerization. The result shows that this catalyst has a high catalytic activity and a good selectivity to isomerization of longifolene. The factors affecting its catalytic activity are investigated. The result also shows that the optimum conditions for the preparation of SO42-/TiO2ZrO2 catalysts are as follows: n(Ti)∶n(Zr)　3∶1, and calcination temperature 550 ℃. Under these conditions, the optimum conditions for isomerization of longifolene are as follows: reaction time 4 h, isomerization temperature 165 ℃, and ratio of solid superacid to longifolene mass part 4 %. Under these conditions, the conversion of longifolene is 99.1 %, and the yield of isolongifolene is 97.2 %. Furthermore,experiments on the  effect of storage time of the catalysts on the reaction and the regeneration of catalysts are carried out.



Key words:  longifolene；isolongifolene；solid superacid；SO42-/TiO2ZrO2 catalyst

歧化松香(丙烯酸-2-羟基乙基酯)酯的合成

林明涛1， 储富祥1*， 马 丽1，2， 周道兵1，王基夫1， 王春鹏1

（1．中国林业科学研究院林产化学工业研究所；国家林业局林产化学工程重点开放性实验室，江苏南京210042； 2．南京林业大学化学工程学院，江苏南京210037）

摘 要： 通过对歧化松香（DPR）分别进行酰氯化和酯化反应成功制备了DPR（丙烯酸-2-羟基乙基酯）酯。考察了反应过程中反应温度、反应时间以及原料物质的量之比对DPR酰氯化反应的影响，确定了DPR酰氯化反应的最佳条件（DPR与三氯化磷（PCl3）的物质的量比为1∶0.33，反应温度50℃，反应时间3h)，并对DPR酰氯的酯化反应进行了研究。实验结果表明：温度对于DPR酰氯化反应的影响较小；而原料物质的量之比对反应程度的影响较大，PCl3用量的增加有利于反应程度的增加。实验结果还显示IR、13C NMR和GC-MS联用分析技术可有效地对反应过程进行跟踪。



关键词： 歧化松香；丙烯酸-2-羟基乙基酯；酰氯；酯化

中图分类号：TQ351.471      文献标识码：A      文章编号：0253-2417(2006)04-0043-05

Study on the Synthesis of Disproportionated Rosin (2Hydroxyethyl Acrylate) Ester

LIN Mingtao1, CHU Fuxiang1, MA Li1,2, ZHOU Daobing1, WANG Jifu1, WANG Chunpeng1

(1. Institute of Chemical Industry of Forest Products,CAF; Key and Open Lab. on Forest Chemical Engineering,SFA,  Nanjing 210042, China；2.College of Chemical Engineering,Nanjing Forestry University, Nanjing 210037, China)

Abstract: Disproportionated rosin (DPR) (2hydroxyethyl acrylate) ester was synthesized by acyl chlorination and esterification of DPR acid. The influences of temperature, reaction time and molar ratio of the reaction were studied by monitoring the course of reaction.The optimum conditions of acyl chlorination and esterification were investigated as follows: molar ratio of DPR to PCl3 1∶0.33, reaction temperature  50℃ and reaction time 3 h. It was found that  temperature had no significant effect on acylation of DPR, and the increase of molar ratio of PCl33 had a positive impact on the reaction degree. The results also showed that IR,13C NMR and GCMS were effective methods for tracking the course of acylation and esterification reaction.



Key words: disproportionated rosin;2hydroxyethyl acrylate;acyl chlorination;

esterification

萜烯马来酸酐催化加氢反应的研究

孔振武1， 汪  浩2， 杜予民2， 储富祥1*

（1.中国林业科学研究院林产化学工业研究所；国家林业局林产化学工程重点开放性实验室，江苏南京210042；2.武汉大学资源与环境科学学院，湖北武汉430072）

摘 要： 研究了反应温度、压力、催化剂用量等因素对萜烯马来酸酐催化加氢制备氢化萜烯马来酸酐合成工艺的影响。实验结果表明，采用钯碳催化萜烯马来酸酐加氢生成氢化萜烯马来酸酐的最佳反应条件为：反应温度150～160℃、氢气压力8～10MPa、催化剂用量4％～6％。该催化氢化工艺具有催化效率高、选择性好、反应时间短等优点。



关键词： 萜烯马来酸酐；催化氢化

中图分类号：TQ351.47      文献标识码：A      文章编号：0253-2417(2006)04-0048-03

Study on Catalytic Hydrogenation of Terpinene Maleic Anhydride

KONG Zhenwu1， WANG Hao2， DU Yumin2， CHU Fuxiang1

(1. Institute of Chemical Industry of Forest Products,CAF；Key and Open Lab. on Forest Chemical Engineering，SFA,Nanjing 210042, China；2.College of Resource and Environment Science, Wuhan University, Wuhan 430072, China)

Abstract: Hydrogenated terpinene maleic anhydride was prepared by catalytic hydrogenation of terpinene maleic anhydride in the presence of Pd/C catalyst.The affecting factors of hydrogenation, such as temperature, pressure and dosage of catalyst,were investigated.Hydrogenated terpinene maleic anhydride could be obtained in a short time with high reaction selectivity and conversion ratio by hydrogenation of terpinene maleic anhydride at reaction temperature from 150 to 160℃,pressure from 8 to 10MPa and the dosage of catalyst from 4 % to 6 %.



Key words:  terpinene maleic anhydride;catalytic hydrogenation

水乳性腰果酚醛树脂的研制

刘月蓉

（福建省林业科学研究院，福建福州350012）



摘 要： 用α-烯基磺酸钠（AOS）与苯乙烯-丙烯酰胺-丙烯酸酯共聚物（BAA）（质量比3∶5）的复配物为乳化剂制备了稳定性高的腰果酚醛树脂乳液。最佳乳化条件为乳化剂用量10％，温度为100～105℃，搅拌速度为800r/min。AOS与BAA复配物对腰果酚醛树脂的乳化效果与其临界胶束浓度（CMC）变化趋势相同,在质量比为3∶5时AOS与BAA的协同作用最大。抄纸时添加0.1 %的含有催干剂的腰果酚醛树脂乳液YGE-8，纸页的干、湿强度分别增加了17.1 %和16.3 %。



关键词： 腰果酚醛树脂;乳化;高分子表面活性剂

中图分类号：TQ322.4      文献标识码：A      文章编号：0253-2417(2006)04-0051-03

Preparation of Cardanol Formaldehyde Resin Emulsions

LIU Yuerong

（ Fujian Institute of Forestry Science, Fuzhou  350012, China）

Abstract: The cardanol formaldehyde resin(CFR) emulsions with high stability were prepared with the mixture ofαolefin sulfonate(AOS) and styreneacrylamideacrylic ester copolymer (BAA) at mass ratio 3∶5 of AOS and BAA.The optimum emulsifying conditions were as follows:dosage of surfactants 10%,temperature 105-115℃, stirring rate 800 r/min.AOS and BAA showed the largest synergitic effect at mass ratio 3∶5. When YGE8 was added at dosage of 0.1 % during formation of paper sheets, the dry and wet strengths of the sheets were increased by 17.1 % and 16.3 %,respectively.



Key words:  cardanol formaldehyde resin;emulsification;polymeric surfactants

纳米微晶纤维素的黏度行为和谱学特征

郭 瑞1，2，丁恩勇1

(1.中国科学院广州化学研究所纤维素化学重点实验室,广东广州510650；2. 中国科学院研究生院，北京100039）



摘 要： 纳米微晶纤维素不但具有纤维素的基本结构与性能，同时又具有纳米微粒的特性，具有广泛的应用价值。通过TEM、X射线衍射、FT-IR对纳米微晶纤维素的形态特点、结构特征及性能特点做了初步探讨，并研究了纳米微晶纤维素胶体的质量分数、温度、剪切速率、pH值、盐质量分数对纳米微晶纤维素胶体黏度的影响。

关键词： 纳米微晶纤维素；黏度；谱学特征

中图分类号：TQ35      文献标识码：A      文章编号：0253-2417(2006)04-0054-03

Viscosity Behavior and Spectral Characteristics of Nanocrystalline Cellulose

GUO Rui1,2， DING Enyong1

（1. Key Laboratory of Cellulose and Lignocellulosics Chemistry,Guangzhou Institute of Chemistry,CAS, Guangzhou 510650, China; 2. Graduate School,Chinese Academy of Sciences, Beijing 100039, China）

Abstract: Nanocrystalline cellulose(NCC) has the backbone of cellulose, composed of β(1→4)Dglucopyranose units, also has many characteristics of nanosize particles which can be used in many fields.The morphological and behavior characteristics of NCC were analyzed by TEM,Xray diffraction and FTIR. The effects of NCC mass fraction, temperature, shearing rate, pH value and mass fraction of salt on the viscosity of colloidal NCC have been studied.



Key words:  nanocrystalline cellulose;viscosity;spectral characteristics

云南3-蒈烯资源的调查研究

耿树香,  尹晓兵,  郑 畹,  武 力

（云南省林业科学院,云南昆明650204）



摘 要： 对云南德宏高含量3-蒈烯思茅松资源调查表明，其林分松脂的3-蒈烯含量为8.52 %～20.11 %,平均含量为19.50%；单株3-蒈烯含量最大值为25.33 %, 高于高山松10.33 %；产品松节油中3-蒈烯含量达11 %以上； 德宏的梁河与潞西林分的3-蒈烯含量平均值分别为8.52 %、20.11 %，3-蒈烯在松节油中的含量的平均值分别为19.47 %和34.88 %；以单株为对象，3-蒈烯最大含量和3-蒈烯在松节油中的含量的最大值分别是27.50%和44.99 %。而其他地区思茅松松脂中3-蒈烯含量则较低，云南松松脂的3-蒈烯含量也相对较低。对这一已成规模的高含量3-蒈烯资源，建议重视开发利用。



关键词： 思茅松；云南松；松脂；3-蒈烯；松节油



中图分类号：TQ351.471      文献标识码：A      文章编号：0253-2417(2006)04-0057-04

Investigation on  Oleoresin Resource of 3Carene in Yunnan Province

GENG Shuxiang， YIN Xiaobing,  ZHENG Wan,  WU Li

(Yunnan Academy Science of Forestry, Kunming 650204, China )

Abstract: Study on the chemical characteristics of oleoresins from Pinus kesiya var. langbianensis in Dehong of Yunnan was carried out by gas chromatography and mass spectrometry.Contents of 3carene in oleoresin are as high as 8.52 %-20.11%,averaging 19.50%. The content of 3carene in oleoresin from one pine is as high as 25.33 %,or 10.33 % higher than that from P.densata oleoresin;The contents of 3carene in turpentine  are over 11 %; The contents of 3carene in oleoresin from Luxi and Lianghe of Yunnan  are 8.52 % and 20.11 % respectively and 3carene contents in turpentine are 19.47 % and 34.88 % respectively.The maximum 3carene contents in oleoresin and turpentine are 27.50% and 44.99 % respectively from one tree. However, 3carene contents are low in oleoresins of P. kesiya var. langbianensis and P. yunnanensis Franch.The resource of oleoresin from P. kesiya var.langbianensis has been exploited on a large scale.Attentions should be paid to the exploitation of P. kesiya var.langbianensis.



Key words:  Pinus kesiya var.langbianensis;P.yunnanensis Franch;oleoresin;

3carene;turpentine

澳洲坚果壳活性炭制备的热解特性研究

宁 平， 杨月红， 彭金辉， 张世敏， 张利波， 陈玉保

（昆明理工大学环境科学与工程学院，云南昆明650093）



摘 要： 以澳洲坚果壳为原料，磷酸为活化剂，利用同步热重-差热分析仪（TG-DTA）对澳洲坚果壳的热失重、热效应以及热解机理进行探讨。实验结果表明:不同条件下的澳洲坚果壳的热分析曲线都有两个失重阶段和相应的吸热峰或放热峰。澳洲坚果壳热解温度在200～410℃之间，800℃时残余量接近零。以磷酸为活化剂浸渍12和24h的磷酸-澳洲坚果壳炭化和活化温度区间为130～400℃, 800℃时残余量分别为34.431 %和17.743 %。磷酸-澳洲坚果壳较佳的活化温度在400℃左右，浸渍时间选择24h为宜。同时随着浸渍时间的增加，DTG峰值温度呈现向低温推移的趋势，由未浸渍的363.63℃降至为243.71℃和238.37℃。磷酸浸渍对澳洲坚果壳有明显促进炭化作用，使其在130℃左右就开始热解炭化，研究结果为澳洲坚果壳活性炭制备提供理论依据。

关键词： 澳洲坚果壳;热分析;热解;活性炭

中图分类号：TQ424.15；TQ91    文献标识码：A    文章编号：0253-2417(2006)04-0061-04

Study on Pyrolysis Characteristics of Macadamia Shell during Preparation of Activated Carbon

NING Ping, YANG Yuehong, PENG Jinhui, ZHANG Shimin, ZHANG Libo, CHEN Yubao

(Faculty of Environmental Science and Engineering,Kunming University  of Science and Technology, Kunming 650093, China)

Abstract: Pyrolysis of macadamia (Macadamia ternifolia F.Muell.)shell with phosphoric acid as activating agent to prepare activated carbon was carried out by simultaneous measurements of thermogravimetry(TG) and differential thermal analysis(DTA),so as to study the pyrolysis mechanism of macadamia shell, the enthalpy change and weight loss. According to experimental data, all thermal analysis curves of macadamia shell have two weight lossstages with related heatabsorption peak or heatreleasing peak under different conditions. Temperature interval of pyrolysis is from 200-410℃,residue amount is close to zero at 800℃. Soaked in phosphoric acid for 12 and 24h, respectively, temperature range of charring and activating of phosphoric acidmacadamia shell is from 130-410℃ and amounts of residue are 34.431% and 17.743 % respectively.The optimum activating temperature is about 400℃,soaking time is 24h by phosphorylation. With increasing of soaking time, peak of DTG curve is gradually shifted to lower temperature,descending from 363.63℃ of the unsoaked to 243.71℃ and 238.37℃ of the soaked.Soaking of phosphoric acid enhances charring reaction and phosphoric acidmacadamia shell starts its  pyrolysis at 130℃.The results provide significant theoretical basis in preparation of activated carbon of macadamia shell.



Key words:  macadamia shell;thermal analysis;pyrolysis;activated carbon

真菌挂膜法处理碱法草浆含氯漂白废水中试研究

胡 笳1，施英乔2，丁来保2，房桂干2*, SIGOILLOT Jeanclaude3

(1．南京林业大学信息科学技术学院，江苏南京210037；  2．中国林业科学研究院林产化学工业研究所；国家林业局林产化学工程重点开放性实验室，江苏南京210042；3．UMR INRAUniversity of Biotechnology,Avenue de Luminy,13288 MARSEILLE Cedex 09,France）

摘 要： 在完成了白腐菌培养的优化条件、系统进行了白腐菌处理碱法草浆含氯漂白废水的实验室试验的基础上，进入工厂废水处理现场，自行设计安装了一套以不锈钢丝为载体、用白腐菌挂膜的生物接触中试反应器，在国内建立了第一个白腐菌处理碱法草浆废液的工厂现场中试基地。中试结果表明，白腐菌对氯漂碱法草浆废水有良好的净化效果。中试系统对碱法草浆废水COD去除率为73.0%～92.2 %，BOD去除率为90.5 %～96.5 %。当水力停留时间（HRT）为24h时，废水只需经白腐菌一步生物处理，COD≤450mg/L，BOD≤100mg/L，SS≤100mg/L，主要指标达到GB 3544-2001国家标准。当HRT为5～10h时，经白腐菌反应器处理再加后续活性污泥法、混凝处理，排放废水各项水质指标均可达到国家标准。



关键词： 白腐菌；漂白废水；化学耗氧量；生物处理；挂膜法

中图分类号：X793      文献标识码：A      文章编号：0253-2417(2006)04-0065-05

Biomembrane Treatment Technology for Straw SodaAQ Pulp Effluent Containing Middlestage Water from Hypochlorine Bleaching

HU Jia1, SHI Yingqiao2, DING Laibao2, FANG Guigan2, SIGOILLOT Jeanclaude3

(1.College of Information Engineering,Nanjing Forestry University, Nanjing 210037, China; 2. Institute of Chemical Industry of Forest Products,CAF; Key and Open Lab. on Forest Chemical Engineering,SFA, Nanjing 210042, China;3.UMR INRA University of Biotechnology,Avenue de Luminy, 13288 MARSEILLE Cedex 09, France )

Abstract: The study on treatment of waste water of straw alkali pulp by white rot fungi has been made systemically in laboratory, the optimization conditions of white rot fungi culture have been given, and the relevant pilotscale equipment of whiterot fungi treatment has been setup first in China. A reactor was used, using stainless steel wire as carrier for biofilm of whiterot fungi. The result of pilotscale experiment showed that the removal rate of COD of straw pulping waste water is 73 %-92.2 %,the removal rate of BOD is 90.5 %-97.8 %, when hydraulic reserved time (HRT) is 24h.The quality of discharged water, by only whiterot fungi biotreatment  was:COD≤450mg/L，BOD≤100mg/L，SS≤100mg/L，pH value 6-9, which meet the requiremenT of the national standard (GB 3544-2001).



Key words:  whiterot fungi;hypochlorine bleaching  effluent；COD；biotreatment；biomembrane treatment

超临界二氧化碳萃取披针叶黄华总生物碱工艺的研究

蔡智慧, 倪传根, 贾瑞琴， 沈敏亮， 王海云

（南京林业大学化学工程学院,江苏南京210037)



摘 要： 利用超临界CO2萃取（SCDE）的方法，研究了披针叶黄华萃取工艺，得到总生物碱。探讨了各种影响因素对披针叶黄华萃取得率的影响，通过正交试验确定了SCDE的最佳工艺为：萃取温度45℃、萃取压力20MPa、CO2流量20kg/h、萃取时间80min。在此条件下，总生物碱得率3.12 %。



关键词： 超临界CO2萃取；披针叶黄华；总生物碱

中图分类号：TQ351.471；O644.2   文献标识码：A   文章编号：0253-2417(2006)04-0070-03

Study on Extraction Technology of Alkaloids from Thermopsis lanceolate by Supercritical Carbon Dioxide

CAI Zhihui, NI Chuangen, JIA Ruiqin, SHEN Minliang, WANG Haiyun

(College of Chemical Engineering,Nanjing Forestry University, Nanjing 210037, China)

Abstract: The needles of Thermopsis lanceolate R.Br. were extracted with supercritical carbon dioxide to obtain alkaloids.Factors affecting extraction yield were discussed. By orthogonal experiments, the optimum technological conditions were: extraction temperature 45 ℃, pressure 20 MPa, flow rate of carbon dioxide 20 kg/h and extraction time 80 min.The yield of alkaloids was 3.12 %.



Key words: supercritical carbon dioxide extraction;Thermopsis lanceolat R.Br;alkaloids

稀土元素改性SO42-/TiO2及其催化合成乙酸松油酯的研究

赵黔榕1, 吴春华2, 毕韵梅1, 张 涛1, 龚 叶1, 佟艳秀1

（1. 云南师范大学化学化工学院，云南昆明650092；2. 西南林学院木质科学与装饰工程学院，云南昆明650224）

摘 要： 用几种稀土元素对单一型固体超强酸SO42-/TiO2进行改性。结果表明，用Ce4+改性效果较好,且当Ce4+质量分数为7.5％、经500℃焙烧3h后催化剂SO42-/TiO2-Ce4+的催化活性最佳，并用TEM、 XRD和IR对其结构进行了表征。该改性催化剂属于纳米级材料，粒径为32nm, 粒度均匀。并以该固体超强酸SO42-/TiO2-Ce4+为催化剂，松油醇和乙酸酐为原料合成乙酸松油酯。利用正交试验得到适宜的合成条件为：反应温度70℃、催化剂用量3％、松油醇与乙酸酐物质的量之比为1∶1.5、反应时间6h。在此条件下，松油醇转化率达99％，产物中乙酸松油酯含量达90％。与普通型固体超强酸进行比较，SO42-/TiO2-Ce4+具有更高的催化活性和选择性。



关键词： 固体超强酸；稀土元素；乙酸松油酯；催化合成

中图分类号：TQ352.71; TQ462    文献标识码：A    文章编号：0253-2417(2006)04-0073-05

Studies on  Solid Superacid SO42-/TiO2 Modified  by Rare Earth Element and Its  Catalysis for Synthesis of Terpinyl Acetate

ZHAO Qianrong1， WU Chunhua2，BI Yunmei1， ZHANG Tao1，GONG Ye1，TONG Yanxiu1

（1.College of Chemistry and Chemical Engineering,Yunnan Normal University, Kunming 650092, China；2.Faculty of Wood Science and Decoration Engineering,Southwest Forestry College, Kunming 650224, China）

Abstract: Common solid superacid SO42-/TiO2 was modified by several rare earth elements. The results showed that Ce4+ was the best modifying agent among these rare earth substances. Ce4+modified solid surperacid SO42-/TiO2Ce4+ displayed excellent activity when superacid SO42-/TiO2 was impregnated by 7.5 % Ce4+ and then calcined at 500 ℃ for 3 h. The structure of SO42-/TiO2Ce4+ was characterized by TEM, XRD and IR methods. The catalyst was a nanomaterial with  uniform granularity of 32 nm. Synthesis of terpinyl acetate from terpineol and acetic anhydride with solid superacid SO42-/TiO2Ce4+as catalyst had been studied for the first time. By orthogonal test, the optimum condition was obtained as follows: reaction temperature 70 ℃, reaction time 6 h, catalyst dosage 3 %,ratio of terpineol to acetic anhydride 1∶1.5. Under this condition, the conversion of terpineol was over 99 %, and the content of terpinyl acetate in the product was 90 %. Compared with common superacid SO42-/TiO2, the modified SO42-/TiO2Ce4+ had higher catalytic activity and selectivity.

Key words: solid superacid;rare earth element;terpinyl acetate;catalytic synthesis

木糖醇发酵菌株固定化细胞的改性研究

林 海， 王申健， 罗 晖， 苗文凭

(北京科技大学土木与环境工程学院，北京100083)



摘 要： 采取了3种不同的方法来改进海藻酸钙微珠的性能，即添加改性剂法、置换法和混合法，考察了改性剂添加量、置换剂浓度、钙化时间以及置换时间对微珠强度的影响。在海藻酸钠与细胞混合液中添加质量分数1.0%的MgO，钙化4 h时固定化细胞的强度最大。该固定化细胞可进行36d共12批次木糖醇发酵，最终木糖醇质量浓度平均值为43.2g/L，木糖醇得率平均值为53.8 %。



关键词： 木糖醇；固定化；海藻酸钙微珠

中图分类号：TQ92      文献标识码：A      文章编号：0253-2417(2006)04-0078-05

Study on Modification of Immobilized Cells for Fermenting Xylitol

LIN Hai, WANG Shenjian, LUO Hui, MIAO Wenping

(School of Civil and  Environmental Engineering,Beijing  University of Science and Technology, Beijing 100083, China)

Abstract: Three different methods, namely, addition, displacement and mixing were adopted so as to improve the strength of calciumalginate beads. The effects of proportions of modifiers, concentration of displacing substance, calcification time and displacing time on the beads were inspected and the strength of immobilized cells reached the maximal value after the mixture of sodium alginate solution and cells was added with mass fraction 1.0 % of MgO and calcified for 4 h. The immobilized cells can be used for the fermentation of xylitol lasting 36 days i.e.12 batches and on average, the final mass concentration of xylitol is 43.2 g/L and the yield of xylitol is 53.8 %.



Key words:  xylitol;immobilization;calciumalginate bead

不同方法提取姜黄色素的研究

李湘洲， 张炎强， 刘艳华， 孙崇鲁

（中南林业科技大学材料科学与工程学院，湖南长沙410004）



摘 要： 用正交试验设计方法分别优化了溶剂回流提取、超声波辅助提取和微波辅助提取3种提取方法中一次提取姜黄色素的最佳工艺条件，对比最佳提取工艺条件下一次提取姜黄色素的得率分别为2.53 %、3.22 %和3.61 %，其一次提取率分别为62.6 %、79.7 %和89.3 %。试验结果表明，微波辅助提取法具有高效、省时等优点，特别适合对姜黄色素的提取。



关键词： 姜黄；姜黄色素；超声波辅助提取；微波辅助提取

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0083-04

Study on  Extraction  of Curcumin by  Different Methods

LI Xianghou， ZHANG Yaniang,  LIU Yanua,  SUN Chongu

(College of Material Science and Engineering,Central South University of Forestry & Technology, Changsha 410004, China)

Abstract: By orthogonal experiment, extraction of curcumin from rhizome of Curcuma longa Linn. with metheds of conventional solvenT, ultrasonic and microwave assisted extraction were studied. Under optimum extraction conditions, the yields of curcumin by these methods were 2.53 %, 3.22 %, 3.61 % with onetime extraction respectively, and the extraction yields were 62.6 %, 79.7 %,89.3 % respectively. Microwave assisted extraction has a bright prospect in the curcumin extraction with the characteristics of considerable time saving and high extraction efficiency.



Key words:  Curcuma longa Linn．；curcumin；ultrasonic extraction；microwave assisted extraction

Studies on Chemical Constituents and Antimicrobial Activities of Persimmon Leaves

JI Zhiping, SU Yinquan*, LÜ Pinghui， Zhang Cunli

(College of Forestry Sciences,Northwest A ＆ F University, Yangling 712100, China)

Abstract: Chemical constituents of persimmon leaves and antimicrobial activities were studied. Results showed that persimmon leaves contained alkaloids, saponins, amino acids, polypeptides, organic acids, phenolic compounds and tannins, saccharides, steroids, flavones, cardiac glycosides, anthraquinones, naphtha, etc. Results of experiments on antibacterial and antifungal activities showed that extracts of alcohol and acetic ester had remarkable bacteriostasis effects against 6 bacteria; aqueous extract was more effective against fungi, and slight against bacteria; petroleum ether extract had no effect against bacteria and fungi; butylalcohol extract had different effects against bacteria, but had no effects against fungi. Results of bacteriostasis activities of acetic ester extract under different concentrations showed that the higher concentration, the stronger bacteriostasis effect was, and that the sequence of bacteriostasis activities was different under different concentrations.

Key words: persimmon leaves;extract;antimicrobial activity

CLC number:TQ91       Document code:A       Article ID: 0253-2417(2006)04-0087-05

柿叶化学成分及其抑菌活性研究

季志平， 苏印泉，吕平会, 张存莉

（西北农林科技大学林学院，陕西杨陵712100）

摘 要：对柿叶的化学成分进行了定性分析和抗菌活性的研究。通过系统预试，初步确定柿叶中含有生物碱、皂苷、氨基酸、多肽、有机酸、酚类和鞣质、糖类、甾体、总黄酮、强心苷、蒽醌、挥发油等物质。抑制活性试验结果显示：乙醇提取物和乙酸乙酯萃取物对供试的6种细菌有较强的抑制作用；水相对供试的5种真菌有较强的抑制作用，而且对细菌有较小抑制作用；石油醚相对真菌和细菌几乎无抑制作用；正丁醇萃取物对细菌有不同程度的抑制作用，而对真菌无抑制作用。用不同质量浓度的乙酸乙酯提取物进行抑菌活性试验，结果显示：质量浓度越高，其抑菌能力越强，而且，在不同质量浓度下，对测试的6个细菌的抑制活性的大小顺序不一致。



关键词：柿叶；提取物；抑菌活性

稻草中密度纤维板用改性脲醛树脂的研究

连海兰1， 尤纪雪2， 周定国1

(1.南京林业大学木材工业学院,江苏南京210037；2.南京林业大学化学工程学院，江苏南京210037)



摘 要： 对比三聚氰胺、二甲基硅油、硅树脂和偶联剂KH-550 四种改性剂改性的脲醛（UF）树脂性能的差别及其对稻草中密度纤维板性能的影响，并进行经济评价，最终确定适用于稻草纤维板的改性UF树脂的工艺条件，同时借助于红外光谱（FT-IR）和差热扫描分析（DSC）研究最佳改性UF树脂的结构和固化特性。结果表明，三聚氰胺改性脲醛(MUF)树脂不论是对树脂性能、板性能改善还是从成本分析方面均为稻草纤维板最佳的胶黏剂，FT-IR显示出与未加三聚氰胺相比,加入三聚氰胺后树脂的羟甲基含量降低了10%，DSC分析则表明其峰值温度有较大幅度的提高，但放出的热量较少。加入三聚氰胺改性的UF树脂其表面张力变小。



关键词： 脲醛树脂；稻草；中密度纤维板；三聚氰胺

中图分类号：TQ91；TQ433.431    文献标识码：A    文章编号：0253-2417(2006)04-0092-05

Study on Modified Ureaformaldehyde Resin for Ricestraw Medium Density Fiberboard

LIAN Hailan1, YOU Jixue2, ZHOU Dingguo1

(1.College of Wood Science and Technology,Nanjing Forestry University, Nanjing 210037, China；2.College of Chemical Engineering,Nanjing Forestry University, Nanjing  210037, China)

Abstract: In order to prepare modified ureaformaldehyde (UF) resin suitable for manufacturing ricestraw medium density fiberboard (MDF),the differences among properties of modified UF resins were investigated, including the influences on the properties of ricestraw MDF bonded with UF resin modified with melamine, KH550, dimethyl silicon oil and silicone resin respectively. The results showed that UF resin modified with melamine (MUF) was effective to bond ricestraw fiber boards, which could improve the properties of board and had an reasonable cost. Analyses by FTIR, UF and MUF resins showed similar curve shapes. MUF resin was waterproof with more amino groups and fewer methylol. DSC results showed that MUF resin demanded higher curing temperature compared to UF resin.The surface tension of MUF resin was 6.3 % less than that of UF resin, hence wetting ability of MUF to straw fiber was improved, which enhanced the diffuse and penetration of the resin into straw fibers and resulted in higher bond strength of the board.



Key words:  ureaformaldehyde resin;ricestraw;medium density fiberboard;melamine

肽类表面活性剂的合成及其表面活性性能的研究

饶小平，宋湛谦*， 高 宏

（中国林业科学研究院林产化学工业研究所；国家林业局林产化学工程重点开放性实验室，江苏南京210042)

摘 要： 以生物质资源棕榈酸、硬脂酸和脱氢枞酸为原料，通过甘氨酸羧基保护法合成了棕榈酰甘氨酸（A）、硬脂酰甘氨酸（B）和脱氢枞酰甘氨酸（C）3种肽类表面活性剂，用IR光谱确证其结构，并对其表面活性性能进行了研究。研究表明：所合成的3种表面活性剂具有良好发泡能力及乳化能力，棕榈酰甘氨酸的表面活性略优于硬脂酰甘氨酸和脱氢枞酰甘氨酸，其泡沫高度可达112 mm，分水时间可达15 min。肽类表面活性剂是一类环境友好的表面活性剂。



关键词： 生物质资源；羧基保护；肽类表面活性剂；环境友好

中图分类号：TQ423       文献标识码：A       文章编号：0253-2417(2006)04-0097-03

Studies on Synthesis and Surfaceactivity of Peptidebased Surfactants

RAO Xiaoping， SONG Zhanqian， GAO Hong

(Institute of Chemical Industry of Forest Products,CAF;Key and Open Lab.on Forest Chemical Engineering,SFA, Nanjing 210042, China)

Abstract: Three peptidebased surfactants including palmitylglycine(A),stearatyl

glycine(B) and dehydroabietylglycine(C) were synthesised from biomass resources of palmitic acid, stearatic acid and dehydroabietic acid respectively through the reaction of carboxylprotecting with glycine. Their structures were characterized by IR spectroscopy. The surfaceactivities of them were also investigated. It has been found that the synthesised surfactants have good foaming power and emulsifying capacity. Palmitylglycine is the best of them, the height of foam can reach 112 mm and wateroil separation time can reach 15 min. Peptidebased surfactants are environmentfriendly.



Key words:  biomass resource;carboxylprotecting;peptidbased surfactant;environmentfriendly

白骨壤酸性多糖的分离纯化及抗补体活性研究

方旭波1, 江 波1*, 王晓岚2

（1. 江南大学食品科学与安全国家教育部重点实验室，江苏无锡214036；2. 江南大学医学系，江苏无锡214036）

摘 要： 采用热水浸提，乙醇沉淀，超滤，三氯乙酸脱蛋白，DEAE-纤维素柱层析脱色，再经DEAESepharose fast flow和Sephacryl S-400层析，从白骨壤树枝分离纯化得到多糖化合物HAM-3-Ⅱb-Ⅱ，经高效凝胶过滤色谱法和比旋光度测定法鉴定为均一性组分，其重均相对分子质量(Mw)为105 200，比旋光度为+27.54°。糖组成分析表明它为酸性杂多糖，主要由半乳糖醛酸、阿拉伯糖、半乳糖和鼠李糖组成。紫外光谱表明其不含核酸和蛋白质等杂质成分；红外光谱证实它是一种酸性果胶类多糖，以α型差向异构为主；补体结合实验表明，该多糖通过经典途径和替代途径共同作用产生显著的抗补体活性, 并呈一定的剂量效应关系。



关键词： 白骨壤;多糖;抗补体活性

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0100-05

Researches on Isolation, Purification and Anticomplementary Activity of Acidic Polysaccharide from the Stems of Avicennia marina (Forsk.)Vierh.

FANG Xubo1, JIANG Bo1, WANG Xiaolan2

(1. The Key Laboratory of Food Science and Safety,Ministry of Education,Southern Yangtze University, Wuxi 214036, China; 2. Medical Faculty,Southern Yangtze University, Wuxi 214036, China)

Abstract: Crude polysaccharides were isolated from the stems of Avicennia marina (Forsk.)Vierh. by hot water extraction and ethanol precipitation.The polysaccharides were further fractioned by ultrafiltration, deproteinated by trichloroacetic acid, decolorized by DEAEcellulose and then isolated by anionexchange chromatography of DEAESepharose fastflow and sizeexclusion chromatography of Sephacryl S400. The purified polysaccharide HAM3Ⅱ bⅡwas proved to be homogeneous by HPGFC and polarimetry.Its molecular weight(Mw)and specific rotation were105 200 and +27.54°respectively. Analysis of monosaccharide composition indicated that HAM3ⅡbⅡ contained high proportions of galacturonic acid, arabinose, galactose and rhamnose, characterizing an acidic heteropolysaccharide. UV spectra of HAM3ⅡbⅡ showed absence of nucleic acid and protein. The characteristic absorptions of IR confirmed the presence of pectic polysaccharide. The measurement of activity was performed by complement fixing test, HAM3ⅡbⅡexpressed potent anticomplementary activity via classical and alternative pathways with the increase proportional to dosage.

Key words:  Avicennia marina (Forsk.)Vierh.;polysaccharide;anticomplementary activity

酸催化的蒸汽爆破预处理强度对麦草酶水解影响的研究

罗 鹏1，2， 刘 忠2， 王高升2

（1.天津商学院机械工程学院，天津300134； 2.天津科技大学材料学院,天津300222）



摘 要： 以蒸汽爆破法对0.5 %的稀硫酸浸渍的麦草进行预处理，研究了不同处理强度对麦草浆得率、半纤维素回收率、纤维素回收率、纤维素酶水解得率产生的影响。实验结果表明，在蒸汽爆破预处理过程中，麦草纤维组分发生分离。随着处理强度的提高，粗浆得率降低，细浆得率上升，纤维素的降解程度和半纤维素的去除程度提高，酶水解得率相应提高。在处理强度为4.14的预处理条件下，半纤维素的水解程度最大，而细浆得率和纤维素的酶解得率最高，分别为62.0%和73.4 %；最佳的处理强度为3.55，此条件下，汽爆麦草原料细浆中的葡萄糖得率和滤出液中总糖的得率最高，分别为20.0%和13.0%。



关键词： 酸催化；蒸汽爆破法；麦草；酶水解

中图分类号：TQ91；Q55      文献标识码：A      文章编号：0253-2417(2006)04-0105-05

Study of Acidcatalyzed Steam Explosion Pretreatment for Enzymatic Hydrolysis of Wheat Straw

LUO Peng1,2, LIU Zhong2, WANG Gaosheng2

（1. College of Mechanical Engineering，Tianjin University of Commerce， Tianjin 300134, China；2. College of Material,Tianjin University of Science and Technology， Tianjin 300222, China）

Abstract: Steam explosions,of different intensities to pretreat wheat straw impregnated in sulfuric acid of 0.5 % concentration were carried out. The effects of pretreatment intensity on total gravimetric recovery, hemicellulosesugar recovery, yield of hemicellulosederived sugars，recovery yield of cellulose, and yield of enzymatic hydrolysis of cellulose were analyzed. Defiberation of wheat straw raw material occurred during steam explosion pretreatment. Total gravimetric recovery decreased and screened gravimetric recovery increased as pretreatment intensity increased. Raising pretreatment intensity led to increase of cellulose and hemi cellulose degradation and enzymatic hydrolysis yield of cellulose. At the condition of pretreatment intensity of 4.14, the hydrolysis of hemicellulose reached the highest degree, the screened gravimetric recovery yield was 62.0 %, the enzymatic hydrolysis yield was 73.4 % .The optimum pretreatment intensity was 3.55, which resulted in the highest glucose recovery of 20.0 % in the water insoluble fiber and the highest total sugars recovery of 13.0 % in the filtrate.



Key words:  acidcatalysis;steam explosion;wheat straw;enzymatic hydrolysis

栀子中三萜酸的提取及结构鉴定

廖晓峰1，2，陈正行1，于 荣2

（1.江南大学食品学院，江苏无锡214036； 2.东华理工学院，江西抚州344000）



摘 要： 对栀子中的主要药用成分三萜酸进行了提取及纯化研究，用95％乙醇，固液比1∶8（kg∶L），在85.4℃回流提取3次，每次2.5 h，浸出率达92.6 %。通过DSC、IR、EI-MS、1H和13C NMR、HPLC等现代分析手段对提取物进行了结构鉴定，证实其为熊果酸，平均含量为0.444 5 %。



关键词： 栀子;三萜酸;熊果酸

中图分类号：TQ91      文献标识码：A      文章编号：0253-2417(2006)04-0110-03

Study on Isolation and Identification of  Triterpene Acid from Gardenia jasminodes  Eills

LIAO Xiaofeng1，2, CHEN Zhengxing1, YU Rong2

(1.College of Food Sciences,Southern Yangtze University, Wuxi 214036, China;2.East  China  Institute  of  Technology， Fuzhou 344000， China)

Abstract: Isolation and purification of triterpene acid from fruit of Gardenia Jasminodes Eills were studied，the optimum processing conditions are: the granularity of powder  0.4 mm, ratio of liquid to solid  8∶1, temperature  85 ℃, 3 times of extraction of 2.5h each, and concentration of alcohol 95 %.Extraction rate of ursolic lixiviate is 92.6 %. Structural identifications by DSC，IR，EIMS，1H and 13C NMR，HPLC show that the triterpene acid is ursolic acid，the average content of ursolic acid is 0.444 5 %。

Key words:  Gardenia jasminodesEills;triterpene acids;ursolic acid

超临界二氧化碳萃取杜仲果实中桃叶珊瑚苷工艺研究

张永康1，2， 胡江宇1， 李 辉2, 欧阳辉3， 银永忠3

（1.吉首大学生物资源与环境科学学院，湖南吉首416000； 2.吉首大学林产化工工程省级重点实验室，湖南张家界427000； 3.吉首大学化学化工学院，湖南吉首416000）

摘 要： 采用超临界CO2流体萃取技术选择适合的夹带剂，进行了从杜仲果实中提取桃叶珊瑚苷的工艺研究。运用L16（45）正交表，较系统地探讨了各因素对提取效果的影响，提取液以Epstahl试剂显色用分光光度法进行分析。研究表明：与传统的溶剂提取法相比，超临界CO2萃取法具有操作简单、活性成分保存好、后续分离易于进行等特点；在萃取中以75％的乙醇为夹带剂，当萃取压力26MPa、萃取温度55℃、分离温度30℃、萃取时间120min、夹带剂用量与原料比6∶1（mL∶g）的条件下，效果最佳，桃叶珊蝴苷得率1.921 %.



关键词： 超临界CO2流体萃取；杜仲果实；桃叶珊瑚苷

中图分类号：TQ91；O69      文献标识码：A      文章编号：0253-2417(2006)04-0113-04

Study on Technology of Extracting Aucubin from Eucommia Fruit by Supercritical Carbon Dioxyde

ZHANG Yongkang1,2, HU Jiangyu1, LI Hui2, OUYANG Hui3, YIN Yongzhong3

(1. College of Biological Resource and Environmental Science,Jishou University, Jishou 416000, China;2. Key Laboratory of Hunan Forest Products and Chemical Engineering,Jishou University, Zhangjiajie 427000, China；3.College of Chemistry and Chemical Engineering,Jishou University, Jishou 416000, China)

Abstract: The technology of extracting aucubin from eucommia ( Eucommia ulmoides Oliv.）fruit was studied using technique of supercritical CO2 extraction with suitable cosolvent. The influence of  extracting factors on extraction effect was studied using orthogonal test table L16（45）. The aucubin content of extracted solutiom was determined by spectrophotometry using chromogenic reaction of Epstahl with aucubin. The study indicates that the technique of supercritical CO2 extraction is better than traditional technique in many respects such as simple operation, good conservation of active component and easy separation. The optimum extraction yield of aucubin is 1.921 % at extracting pressure 26 MPa, extracting temperature 55 ℃,separation temperature 30℃, extracting time 120 min, and ratio of cosolvent (75 % alcohol) with raw materials 6∶1(mL∶g).



Key words:  supercritical CO2 extraction;eucommia fruit;aucubin

纤维素超临界水解反应的研究进展

汪利平1，2， 吕惠生1， 张敏华1*

(1.天津大学石油化工技术开发中心绿色合成与转化教育部重点实验室，天津300072；2.中国石油兰州润滑油研究开发中心，甘肃兰州730060)

摘 要： 从纤维素超临界水解反应的反应产物、反应机理和反应动力学等方面，对纤维素超临界水解反应的研究进展进行了综述；与传统的酸水解和酶糖化工艺比较，纤维素超临界水解工艺具有效率高、过程简单和环境友好等技术特点；展望了纤维素水解反应技术的应用前景。

关键词： 纤维素；超临界水；水解反应

中图分类号：TQ35      文献标识码：A      文章编号：0253-2417(2006)04-0117-04

Progress of Research on Cellulose Hydrolysis in Supercritical Water

WANG Liping1,2， LÜ Huisheng1， ZHANG Minhua1

（1.Key Lab for Green Chemical Technology of State Education Ministry；Tianjin R & D Center for Petrochemical Technology, Tianjin University, Tianjin 300072, China； 2.PetroChina Lanzhou Lubricating Oil R & D Institute, Lanzhou 730060, China）

Abstract: Hydrolysis of microcrystalline cellulose in supercritical water was reviewed. The main reaction pathway, reaction mechanism and reaction  kinetics  were described on the basis of detailed product analyses. Compared with traditional technologies of acid hydrolysis and enzymatic saccharification, the technology of supercritical hydrolysis has the advantages of high efficiency, simple processing and environment friendly. The application prospect of this technology is described.

Key words:  cellulose;supercritical water;hydrolysis

超临界二氧化碳萃取牛至挥发性组分的研究

车国勇1，2, 庞 浩1, 廖 兵1*, 张镜澄1

(1.中国科学院广州化学研究所；中国科学院纤维素化学重点实验室，广东广州510650；2.中国科学研究院研究生院，北京100039)

摘 要： 采用GC-MS技术对在超临界CO2中加入夹带剂萃取牛至的萃取物的化学成分进行了分析，共鉴定出20种化合物。同时与水蒸气蒸馏产物的组成进行了比较。结果发现在超临界萃取中加入夹带剂所得精油得率明显高于水蒸气蒸馏的精油得率；夹带剂极性越大，萃取物得率越多，抗氧化剂的量也越多。



关键词： 超临界CO2；夹带剂；牛至精油；抗氧剂



中图分类号：TQ91；TQ654.1     文献标识码：A     文章编号：0253-2417(2006)04-0121-03

Study on Extracting Volatile Components from Oregano by  Supercritical CO2

CHE Guoyong1,2, PANG Hao1, LIAO Bing1, ZHANG Jingcheng1

(1.Guangzhou Institute of Chemistry；Key Laboratory of Cellulose and Lignocellulosics Chemistry,Chinese Academy of Sciences, Guangzhou 510650, China; 2.Graduate School of Chinese Academy of Sciences, Beijing 100039, China)

Abstract: Volatile extract was obtained from oregano (Origanum vulgare L.) by supercritical CO2 extraction with cosolvent. The chemical composition of the extract of oregano was studied by GCMS technique, 20 compounds were identified. The extract was compared with the essential oil gained by hydrostillation. The results showed that the content of oregano essential oil by supercritical CO2 extraction with cosolvent was obviously higher than that by hydrostillation. The greater the polarity of cosolvent is, the higher is the content of antioxidant.



Key words:  supercritical CO2;cosolvent;oregano essential oil;antioxidant

GC-MS分析确认诺卜乙基醚氧化反应产物的结构

陈金珠1， 肖转泉2， 王宗德3

(1. 江西农业大学理学院，江西南昌330045； 2.江西师范大学化学化工学院，江西南昌330027； 3. 江西农业大学林学院，江西南昌330045)

摘 要： 通过GC-MS分析，确认了高锰酸钾碱性溶液氧化诺卜乙基醚反应产物中6个主要产物的结构，它们是： 2,2-二甲基-3-（β-乙氧基丙酰基)环丁酮、cis-2,2-二甲基-3-（β-乙氧基丙酰基)环丁烷乙酸、3-羟基-cis-2,2-二甲基-3-（β-乙氧基丙酰基)环丁烷乙酸、2,3-二羟基诺卜乙基醚、1-羟基-cis-2,2-二甲基-3-（β-乙氧基丙酰基)环丁烷乙酸、5-羟基-2,3-环氧诺卜乙基醚。



关键词： GC-MS分析；诺卜乙基醚；氧化产物



中图分类号：TQ351.472;O624    文献标识码：A    文章编号：0253-2417(2006)04-0124-04

Structural Identification of the  Oxidation Products of Nopyl Ethyl Ether by GCMS

CHEN Jinzhu1, XIAO Zhuanquan2,  WANG Zongde3

(1. College of Science,Jiangxi Agricultural University, Nanchang 330045, China;2. College of Chemistry and Chemical Engineering,Jiangxi Normal University, Nanchang 330027, China; 3. College of Forestry,Jiangxi Agricultural University, Nanchang 330045, China)

Abstract: Nopyl ethyl ether was oxidized in alkaline potassium permanganate solution, and the structures of 8 main products were identified by GCMS, which are 2,2

dimethyl3(βethoxypropionyl)cyclobutanone,cis2,2dimethyl3(βethoxypro

pionyl)cyclobutaneacetic acid, 3hydroxycis2,2dimethyl3(βethoxypro

pionyl) cyclobutaneacetic acid, 2,3dihydroxynopyl ethyl ether,1hydroxycis

2,2dimethyl3(βethoxypropionyl) cyclobutaneacetic acid and 5hydroxy2,3

epoxynoyl ethyl ether.



Key words:  GCMS;nopyl ethyl ether;oxidation products